AMBEX RP-5

(Nitrite Free)

AMBEX RP-5 is a mildly alkaline liquid material that is diluted with water for rust inhibiting of ferrous alloys.  It contains no nitrites.  AMBEX RP-5 provides a thin dry film on ferrous alloys to protect them from rusting or oxidation during temporary storage or handling.

AMBEX RP-5 is ideally suited for use on components of complicated geometries that cannot be thoroughly rinsed with water, especially where residual water may cause rusting.

AMBEX RP-5 provides protection against rusting after aqueous cleaning operations and prevents rusting of components during temporary storage and handling.  AMBEX RP-5 promotes drying by facilitating the reduction of water on the surface and internal cavities of components.

# OPERATING PARAMETERS

Concentration:  Use 1 ½ to 3% by volume

Temperature:  170°-190°F  (77°-88°C)

Time:  1 – 5 minutes

# MAKE-UP

Slowly add the required concentration of AMBEX RP-5 to the desired volume of warm water (110°F/43°C) and mix thoroughly.  Heat to recommended operating temperature range.

## OPERATION

Immerse the clean and thoroughly rinsed components completely into the AMBEX RP-5 operating solution.  Gently agitate the components to insure complete wetting of surfaces and internal cavities.  Allow the components to remain in solution for the required time.  Clean, filtered, dry air may also be used to blow-off any excess or residual water.

NOTE:  An invisible protective film that will inhibit rusting in mild industrial environments will remain on the components after processing in AMBEX RP-5.  However, this protection should no be compared to that of rust preventative oils or a preventative compound such as AMS 3065.

AMBEX RP-5 is designed to be a temporary rust inhibitor, providing protection between various finishing or repair operations, as well as in short term storage.

EQUIPMENT

AMBEX RP-5 solutions may be contained in stainless steel or polypropylene    tanks.  The solution is best heated by the use of stainless steel coils.  Although AMBEX RP-5 DOES NOT give any toxic fumes, ventilation is recommended to remove vapors given off by heating of the solution.

CONTROL

AMBEX RP-5 does not require any complicated chemical analysis to control the solution.  Simply add back AMBEX RP-5 made up to the original make-up concentration (e.g. 2% by volume), when the operating solution level drops below the original volume level due to drag-out or evaporation.

WASTE TREATMENT

AMBEX RP-5 solutions are slightly alkaline.  They contain no nitrites.  They must be neutralized prior to discharge into a waste treatment system.  Consult local, state, and federal regulations regarding effluents.

PRECAUTIONARY INFORMATION

Hazards:  AMBEX RP-5 is slightly alkaline, and contact of the skin or eyes with the hot solution could cause burns and irritation.

First Aid:  In case of contact with eyes or skin with AMBEX RP-5 solution, flush areas affected with clean, cool water for at least 15 minutes; for eyes, seek immediate medical attention.  Remove contaminated clothing or shoes and wash before reuse.

Handling:  When making up solutions or adding AMBEX RP-5 to operating solutions be certain that cool water is used or the operating solution is at ambient temperature (70°F or less).

Add AMBEX RP-5 slowly and cautiously.  Do not get on skin or eyes.  DO NOT TAKE INTERNALLY.  Wear protective clothing, rubber gloves and chemical safety goggles.

Keep containers tightly closed and store indoors in cool dry place.  Do not reuse containers and wash before disposal.