AMBEX AS-1

AMBEX AS-1, A WATER-SOLUBLE DRY ACID POWDER, IS A CAREFULLY BALANCED MIXTURE OF ACID SALTS, ACTIVATORS AND SURFACE ACTIVE AGENTS.  IT HAS BEEN USED TO REPLACE MOST OF THE COMMONLY USED PLATING ROOM ACIDS.  A TYPICAL RANGE OF CONCENTRATION OF ACID WHICH AMBEX AS-1 HAS BEEN USED TO REPLACE IS FROM 1% SULFURIC TO AS HIGH AS 50% MURIATIC.

BETTER ADHESION, BRIGHTER ELECTRO DEPOSIT WITH AMBEX AS-1

Ambex As-1 gives cleaner, brighter, smut-free steel surfaces and therefore plated deposits are brighter and adhere better.  Because of this brighter and cleaner surface, shorter plating times may be used to get equivalent final brightness.  Plated surfaces are more uniform and have better depth of color when Ambex AS-1 is used as the acid dip before plating.

On wire goods, the problem of differential color, due to poor wire, is solved by using Ambex AS-1 in the preparation of the metal prior to plating.

SAFETY AND WORKING CONDITIONS

The hazards of handling liquid acids are eliminated when Ambex AS-1 is used.  Safety committees have recommended using dry acid salts whenever possible.  Special acid storage is not required for Ambex AS-1.  There is no possibility of acid spillage.  The only handling equipment required for charging a tank is a shovel.

Working conditions in the plating room are greatly improved when switching to Ambex AS-1 because this material does not give off typical acid fumes.  Plating room haze is completely eliminated when using Ambex AS-1.  Room temperature operation of Ambex AS-1 does not require ventilation.  These features mean better working conditions and no acid fumes or rusting of equipment or work in process.

USER BENEFITS WITH AMBEX AS-1

Feature	Benefit

Dry acid salt packed in fiber drums	No carboys to return - no breakage - no special storage space required - no possibility of acid spillage - no dangerous acids to handle - no special equipment necessary other than a shovel.  These benefits all mean lower handling costs and happier help.

No hazard in handling a dry salt	Less skilled help can make up acid tanks with no danger - no accidents - less loss time - lower costs.

Non-fuming	No ventilation required for room temperature operation - Plating equipment and adjacent equipment and work in progress will not be corroded.

Less contamination of plating solutions

due to cleaner, smut free surface	Plating solutions will not have to be carbon treated as often with resultant savings in brighteners and labor.

FOR ACID DIPPING

Ambex AS-1 dissolved in water is used as an activating acid dip prior to electroplating the following basis metals:

Steel	Zinc Base Diecastings

Cast Iron	Aluminum

Malleable Iron	Nickel Silver

Brass	Pewter

Copper	Lead Alloys

Beryllium Copper	Stainless Steel

FOR PICKLING TO REMOVE OXIDES, RUST, HEAT TREAT OR WELDING SCALE

As an acid dip material, Ambex AS-1 solutions are usually used at room temperature.  However, many applications of this material to remove oxides, rust, heat-treat or welding scale will require heat.  Temperatures up to 130ºF will accelerate the action in these pickling type jobs.  Cathodic current can be used very effectively for some more difficult cases of oxide or scale removal.  PR current has also been used.

NICKEL ACTIVATION

Ambex AS-1 will activate passive nickel.  Thus when plating chromium over nickel, the use of Ambex

AS-1 in the acid dip will improve the chrome coverage.

CHROME STRIPPING

Ambex AS-1 in hot solution is being used as a chrome plate strip. It is fast, strips without producing smut, and will not attack the under plated nickel.  When chrome is stripped from nickel with Ambex AS-1 the parts may be replated without further activation.

TYPICAL APPLICATIONS OF AMBEX AS-1

APPLICATION	CONC                    TEMP                TIME

Acid dip on steel before bright plate on

full automatic	1#/gal	Room	15 seconds

Acid dip on steel before phosphating

Note:    Finer grained phosphate	2#/gal	Room	1 - 3 minutes

coating, use less primer, paint.

Acid dip on zinc die castings before

bright copper on full automatic plating	4 oz/gal	Room	15 seconds

machine.

Acid dipping copper plated zinc die

castings before nickel and chrome.	8-16 oz/gal	Room	10 - 60 seconds

Note:  Easier to make up, no fumes,

longer life.

Acid dipping brazed tubular steel before

plating.  Note:  Cleans brazed areas better.	1#/gal	Room	30 seconds

Steel stampings before nickel and chrome	1#/gal	Room	90 seconds

Chromating zinc diecastings	8 oz/gal	Room	10 - 30 seconds

Acid dip steel before zinc plate	2#/gal	120ºF	30 seconds

APPLICATION	CONC                    TEMP                TIME

Pickle steel after heat treating	2#/gal	130ºF	varies

Chromium stripping.	1-2#/gal	180ºF	1 - 3 minutes

Nickel Activation.	1#/gal	120ºF	1 minute

Acid dip for buffed brass before

bright nickel and chrome.	8-16 oz/gal	Room	10 - 60 seconds

OPERATING CONDITIONS AND EQUIPMENT

Concentration...............................................................................1 - 3 lbs/gal

Temperature.................................................................................Room to 130ºF

Tank..............................................................................................Koroseal, rubber, polyethylene, PVC or

lead lined.

Heating Coil...................................................................................Karbate, Graphite or Chemical Lead.

Electrodes......................................................................................Chemical lead, Graphite, Type AGX58

or Carbon type GA available from

National Carbon Co., PO Box 6087,

Cleveland, OH

SUGGESTED CYCLE FOR STEEL

- Electroclean - Ambex AF, 8 to 12 oz. per gal., 6 volts, work as anode, 180º to 200ºF, 1 - 3 minutes.

- Water rinse.

- *Ambex AS-1, 1 to 2 lbs./gal., room temperature, **1/2 -1 minute.

- Water rinse.

- Electroclean - Ambex AF, 8-12 oz./gal., 6 volts, work as anode, 180º - 200ºF, 1 - 3 minutes.

- Water rinse.

- *Ambex As-1, 1 to 2 lbs./gal., room temperature, 1/2 - 1 minute.

- Water rinse.

- Electroplate, nickel, white brass or other.

*For eliminating the differential color on plated wire goods, make the work the cathode (direct) in Steps No. 3 and/or 7 above.  Current optional on step 7 may be necessary in extremely stubborn cases.  Use a potential of 6 volts.  Carbon anodes are preferred, but chemical lead may be used if necessary.

**Work with heat treat scale, welding scale or other oxide coatings may require higher temperatures

(120º to 130ºF).

Increasing the concentration of Ambex AS-1 to 2 - 3 lbs./gal. or raising the temperature accelerates the pickling action.

SUGGESTED CYCLE FOR BRASS AND COPPER

- Electroclean - Ambex 22, 6 - 8 ozs./gal., 4 - 5 volts, work as anode, 180º - 200ºF, 1/2 - 1 minute.

- Cold water rinse.

- Ambex AS-1, 8 - 16 ozs./gal., room temperature, 1/2 - 1 minute.

- Cold water rinse.

- Electroplate.

SUGGESTED CYCLE FOR ZINC BASE DIECASTINGS

- Electroclean - Ambex 22, 8 ozs./gal., 4 - 6 volts, work as anode, 180º - 200ºF, 1/2 to 1 minute.

- Cold water rinse.

- Ambex AS-1, 4 - 8 ozs./gal., room temperature, 15 - 30 seconds.

- Cold water rinse.

- Electroplate.

CONTROL PROCEDURE

Ambex AS-1 may be controlled by titration.

BY TITRATION

- Pipette a 10 ml. sample into a 250 ml. Erlenmeyer flask.

- Add 25 ml. of distilled water, 5 - 10 drops Bromocresol green indicator and titrate with 1 Normal Sodium Hydroxide until the solution turns a blue-green color.

- Calculation:  ml. of 1N Sodium Hydroxide x 1.94 = oz/gal. Ambex AS-1.

CAUTION

Solutions of Ambex AS-1 should be handled like other acid.  Avoid skin and eye contact.  Flush exposed areas immediately with clean cold water.  Wear goggles and protective clothing  Consult a doctor immediately in case of injury.

- The information contained herein is based on our experience and to the best of our knowledge is true and accurate.  However, since the conditions for use of the products described are often beyond our control, both the information and products are offered without warranty or guarantee as to such use and nothing herein shall be construed as a recommendation to use any product in violation of any patent rights.