TECHNICAL INFORMATION DATA SHEET

AMBEX 111S
WARNING!!!  Do not attempt to use this product without reading this bulletin and the Material Safety Data Sheet.

An alkaline tumbling compound used to clean, bleach, and shine roll steel parts.
Ambex 111S is a highly alkaline barrel and vibratory finishing compound for steel and stainless steel.  It is specially formulated to remove oil, light rust or scale and produce a moderate polish in one step.

Ambex 111S is used at 2-5 oz/gal (15-40 G/Lit) depending upon the condition of the work.  For barrel finishing the solution should cover the work by 1-2 inches (2-5 cm).  In flow through vibratory machines, Ambex 111S can be used at 2 oz/gal (15 G/Lit) of pre-mixed solution at a rate of 5 gal/hr/cu ft (1 Lit/Hr/DM³) of load.  At the end of the cycle (15-45 minutes depending upon condition) parts should be flushed with clean water and dried.

Parts may also be given a slight radius or light deburring by tumbling with small size deburring medial with Ambex 111S all in a single step.

CAUTION:
Ambex 111S is a highly alkaline material and should be handled with the same precautions as for Caustic Soda.  Avoid contact with skin or eyes.  In the event of contact with the skin, flush thoroughly with water.  For eyes, flush thoroughly with water and get medical attention.

WASTE DISPOSAL INFORMATION:
Ambex 111S solutions may be discarded by neutralizing the alkaline content in accordance with locally acceptable standards for effluent pH.  Total alkalinity to a phenolphthalein endpoint is 47% w/w/ as Na2O.  Ambex 111S contains no chromates, cyanides, fluorides, phosphates, silicates, or phenolic compounds.  All surface active agents are biodegradable.
