# AMBEX 0620

AMBEX 0620 IS AN ALKALINE, NON-CYANIDE, NON-PHOSPHATE CLEANER AND ELECTROACTIVATOR FOR ALLOY STEELS, MARTENSITIC AND FERRITIC IRON BAS ALLOYS, AUSTENITIC IRON BASE ALLOYS, NICKEL AND COBALT BAS ALLOYS AND TITANIUM.

AMBEX 0620 REMOVES OXIDES, SCALE, CARBON SMUT AND LIGHT SOILS AND ENSURES EXCELLENT ADHESION OF SUBSEQUENT PLATED DEPOSITS.

AMBEX 0620 CONTAINS NO CYANIDE OR PHOSPHATES AND IS BIODEGRADABLE SO WASTE TREATMENT IS SIMPLIFIED.

AMBEX 0620 CAN BE USED AS A SOAK CLEANER, ELECTROCLEANER OR AN ELECTROACTIVATOR IN CONJUNCTION WITH PERIODIC REVERSE CURRENT CLEANING.

OPERATING CONDITIONS:

### CONCENTRATION:	16-24 OZ/GALLON

TEMPERATURE:	100-120F (38-49C)

CURRENT DENSITY:	25-100 asf

VOLTAGE:	6-9 VOLTS

PERIODIC REVERSE:	7-10 SECONDS ANODIC

3-5 SECONDS CATHODIC

NOTE:  AMBEX 0620 CANNOT BE USED ON ALUMINUM OR OTHER HIGH ALKALINE SENSITIVE METALS.

Page 1

AMBEX 0620 TITRATION VALUES:

- PIPETTE A 10 ML ALIQUOT OF TEST (WORK) SOLUTION INTO A 250 ML                            ERLENMEYER FLASK.

- DILUTE TO 200 ML W/DISTILLED WATER.

- ADD 5 OR 6  DROPS OF PHENOLPHTHALEIN INDICATOR SOLUTION AND SWIRL TO PRODUCE PINK COLOR.

- TITRATE WITH 1N HYDROCHLORIC ACID TO CLEAR END POINT.

- CALCULATION OF OZ. PRODUCT/GAL.:

# ML’s 1N HYDROCHLORIC ACID X .72 = OZ./GAL.

HANDLING PRECAUTIONS:  AMBEX 0620 CONTAINS MORE THAN 50% SODIUM HYDROXIDE AND IS THEREFORE A HIGH ALKALINE CHEMICAL AND SHOULD BE HANDLED ACCORDINGLY.  AVOID SKIN, ORAL, AND EYE CONTACT.  PROTECT EYES WITH GOGGLES AND SKIN WITH GLOVES AND OTHER ALKALINE RESISTANT PROTECTIVE CLOTHING.  IN CASE OF CONTACT, FLUSH EXPOSED AREAS IMMEDIATELY WITH COPIOUS AMOUNTS OF CLEAN COLD WATER.  CONSULT A DOCTOR AT ONCE IN CASE OF INJURY.

OUR RECOMMENDATIONS ARE MADE IN GOOD FAITH, AND ARE BASED ON OUR SKILL AND EXPERIENCE.  HOWEVER, SINCE THE CONDITIONS OF USE OF THESES PRODUCTS ARE BEYOND OUR CONTROL, THIS INFORMATION IS GIVEN ON THE XPRESS CONDITION AND AGREEMENT THAT AMBION CORPORATION OR ANY OF ITS AGENTS, WILL NOT BE LIABLE TO ANY PERSON BY REASON THEREOF.  NOTHING HEREIN SHALL BE DEEMED TO BE A RECOMMENDATION TO USE ANY PRODICT IN VIOLATION OF ANY EXISTING PATENT RIGHTS.

Page 2