Ambion Corporation	Telephone:  203-723-1437

37 Naugatuck Drive	Fax:  203-723-0101

Naugatuck, CT 06770	Email:  customer.service@ambionchem.com

TECHNICAL INFORMATION DATA SHEET

AMBEX 223LF

NON-CORROSIVE LIQUID CLEANER

For commercial and industrial use only

Refer to MSDS before using

Ambex 223LF is a general purpose, non-alkaline, liquid cleaning compound designed mainly for the removal of oil from metallic surfaces during the fabrication process.  It is safe for use on almost all metals including aluminum, zinc, iron copper and related alloys.  It is recommended for cleaning situations involving combinations of metals, for white metal and for solder.  It is 100% biodegradable.  Ambex 223LF produces very little foam under conditions of high agitation and therefore may be used in spray and scrub cleaning applications.  It is extremely effective in removing difficult greasy and oily soils such as lard oil as well as buffing compounds and therefore is also recommended for soak and ultrasonic cleaning.  It is used at low concentrations and is remarkably long lived.

Properties:

Density (lb./gal.) 	8.66

Appearance	pale yellow syrup

Odor	slightly sweet, musky

Flash Point	none

pH	8.4

Use:

Ambex 223LF should be used at dilution rate of 2 to 6% by volume of water.  The resulting solution may be used for cleaning at any temperature that is suitable for the situation.  Generally, the cleaning ability of the solution improves as the temperature is increased.  Temperatures between 130°F and 200°F are generally recommended.  Use of ultrasonic cleaning will improve performance and allow for lower concentrations and temperatures.  The solution is applied to the work to be cleaned by immersion, scrubbing or high pressure spray.  After cleaning a water rinse will remove cleaner residue.  Electro- cleaning should subsequently be employed before electroplating.  Because of the mild nature of the product, equipment constructed of almost any material may be used if it tolerates the operating temperature.

Handling:

Ambex 223LF will normally not be irritating to the skin.  It can cause eye irritation.  Operators should wear suitable eye protection.  In the event of skin contact, remove contaminated clothing and rinse the affected area with plenty of water.  In the case of eye contact, wash eyes with lots of water for 15 minutes.  If irritation persists, get immediate medical attention.  Under anticipated use conditions, the material does not normally present any health hazard associated with inhalation.