Asia Pacific (AUST) International Trading Pty Ltd

High grade quality Brazil Iron Ore from Vale

Guaranteed Specification

Fe                64.5%                     Rej: 63.5%

Al2O3           3.5% Max

SiO2             3.5% Max

S                  0.008% Max

P                   0.008% Max

Physical Characteristics

<0.15mm        15%max

>10mm            15%max

Moisture 8.00% at 105 degrees C

Price information:

$85 per dry Metric Ton, up to 1000,000 Tons per month. Available July 2009.

Delivery Schedule:

30/40 days CFR for AWSP after receipt of the Buyer's Bank Irrevocable DL/C at Sgith.

Inspection:

Quality, Quantity Weight by SGS or equivalent Seller's cost at loading port.

Payment Terms:

The payment will be made by open confirmed, irrevocable, transferable DLC (Documentary Letter of Credit). One for each month of shipment, at the value of 100% of the total of shipments amounts of that month.

The Seller will withdraw 100% of the value on presentation of all shipment documents, month by month.

Contract Term:

12 months to 60 months.