AMBEX 16H

AMBEX 16 is an essentially neutral, liquid compound which will produce a high, bright, mirror-like luster on aluminum, brass, copper, gold, silver, and zinc base.  It will not  produce after-corrosion on zinc base parts and will prevent the tarnishing of brass during long-time burnishing operations.  Ambex 16 produces excellent results in soft or hard water.

OPERATING CONDITIONS:

Concentration:  4 oz./ft. sq. (4 ml/dm sq.)

Temperature:    Ambient

Ambex 16H is used at above concentration of mixed load with sufficient water to cover the work.  Parts should be clean and free of oil, dirt and tarnish and the steel shot should be clean and highly polished.

After burnishing, the barrel should be drained and the work separated from the shot.  Return the shot to the barrel and rinse the work in baskets.  If the shot is to be stored overnight or over a weekend, cover the shot with water and add a normal charge of Ambex 16H.  Tumble for a few minutes to thoroughly mix the compound with the water.  This will prevent the shot from rusting or dulling.

CHEMICAL PROFILE:

pH of working solution   9.0

Phosphate free              Yes

Attack on metals at recommended operating conditions

Zinc & Copper – No Attack

Brass               - No Attack

Zinc                  - No Attack

Aluminum         - No Attack

PHYSICAL CHARACTERISTICS:

Physical Appearance      Liquid

Flash Point                      None

Foaming Tendency         Low

CAUTION:

While Ambex 16H is essentially non-hazardous, continued exposure of unprotected skin to the concentrate or use solutions may have a defatting action on the skin and cause chapping and/or irritation.  Avoid contact with skin or eyes.  In the event of contact with the skin, flush thoroughly with water.  For eyes, flush thoroughly with water and get medical attention immediately.

continued...

WASTE DISPOSAL INFORMATION:

Ambex 16H contains no chromates, cyanides, fluorides, phosphates, silicates or phenolic compounds.  All surface active agents are completely biodegradable.

The use, handling, and storage of this product may involve certain hazards.  Please refer to the Material Safety Data Sheet for additional hazard information.

The information presented herein was prepared by technically knowledgeable personnel and to the best of our knowledge is true and accurate.  It is not intended to be all-inclusive, and the manner and conditions of use and handling may involve other or additional considerations.