TECHNICAL INFORMATION DATA SHEET

AMBEX WOF

# Chemical Cleaning Compound

WARNING!!!  Do not attempt to use this product without reading this bulletin and the Material Safety Data Sheet.

Ambex WOF is a powdered, alkaline cleaning compound for ferrous and copper surfaces.  It is used primarily to remove oily soils from metal fabrications prior to other finishing operations.  It rapidly and efficiently removes grease, oils and smudges.  No etching or pitting of the base metal will occur. This product may be used in a soak tank or in tumbling operations.

It may be used to clean aluminum but some metal attack can occur at higher temperatures and concentrations.  Because of foaming, this product is not recommended for use in spray applications.

DIRECTIONS:  Use at about 4 - 6 oz. per gallon of water at 150°F to 170°F in steel soak tanks.  Cleaning time will vary, usually between 1 and 5 minutes. In tumbling operations, use with hot water at about 2 - 3 oz. per gallon of water.  For aluminum, use at 1 – 2 oz. per gallon.

PRECAUTIONS:  Ambex WOF is an alkaline material and is corrosive to eyes.  Always wear chemical worker’s goggles when handling it.  Rubber gloves and aprons should also be worn.  Wash facilities for skin and eyes should be present in the immediate work area.  Refer to the Material Safety Data Sheet before attempting to use this material.