AMBEX 901

Ambex 901 is a powdered, mildly alkaline product which was developed to be used as an electro cleaner for brass alloys, copper and zinc die cast.

OPERATING CONDITIONS:

Concentrations:                     8-12 ozs./gal.

Temperature:                        160F-180F

Time:                                     1-3 minutes

Polarity:                                 Anodic

Equipment:                            Mild steel tanks, coils and anodes

Ventilation:                             Recommended

MAINTENANCE NOTE FOR ELECTROCLEANER:

When recharging the tank with a fresh solution, be sure that the cathodes are free of sludge and that the bus bars are bright and clean.  Sludged cathodes and dirty bus bars act as insulators, which will consequently reduce the current density.

TITRATION PROCEDURE:

Factor   (oz./gal.)   0.6

Factor   (gms./l.)    4.5

- Pipette 10 mls. of Ambex 901 solution into 250 ml. Erlenmeyer flask.

- Add 100 mls. of water and 4 to 5 drops Phenolphthalein indicator.

- Titrate with 0.5 N Hydrochloric Acid until the solution turns to a clear end point.

- Record mls. of 0.5 N Hydrochloric Acid used.

Ambex 901 does not contain any chelators and is a completely biodegradable product.

CAUTION:

Ambex 901 is an alkaline product that should be handled accordingly.  Avoid skin and eye contact.  Wear protective clothing, gloves and goggles.  Flush exposed areas immediately with clean, cold water.  In case of injury contact a physician immediately.