Ambion Corporation

37 Naugatuck Drive

Naugatuck, CT  06770

(203)723-1437

(203)723-0101

AMBEX 315DX

AMBEX 315DX is a dry powdered, non-chromated acid deoxidizer and desmutter for wrought and extruded aluminum alloys.

USEAGE:  16 OZ/GAL (120 G/LIT)

IMMERSION TIME:  15 SECONDS TO 2 MINUTES

EQUIPMENT:  Polyethylene, PVC, or polypropylene (or plastic lined steel tank).

HEATER COILS:  Should be either carbon or Teflon.

CAUTION:  AMBEX 315DX is an acid powder and contains fluorides.  Avoid contact with skin or eyes.  In the event of contact with the skin, flush thoroughly with water.  If redness or irritation develops, or skin whitens noticeably, get medical attention and inform physician of presence of fluorides.  In the even of contact in the eyes, flush thoroughly with water, and get medical attention.  Inform physician of presence of fluorides.

WASTE DISPOSAL INFORMATION:  AMBEX 315DX may be discarded by neutralizing the acid content to locally acceptable standards for effluent pH.  Removal of metal hydroxides may be necessary due to local restrictions.  Total fluoride content id 3%.  AMBEX 315DX contains no chromates, cyanides, phosphates, silicates or phenolic compounds.