AMBEX E-1000

Ambex E-1000 is a granular, alkaline etchant designed specifically for etching aluminum with a minimum of fuming and foaming.  Ambex E-1000 forms a stable controlled foam blanket which entraps caustic spray resulting from hydrogen evolution.  Ambex E-1000 can be mixed with conventional etchants to provide a controlled foam blanket where desired.  All surfactants are biodegradable.

Ambex E-1000 provides an outstanding sequestering action that prevents sludging and sealing of heating coils and tank walls.  This eliminates the need for expensive descaling of tank and heating coils and assures the most efficient heating.

HANDLING INSTRUCTIONS:

Ambex E-1000 contains highly alkaline materials.  Contact with skin or eyes may cause irritation and burns.  The same safety precautions should be observed as when handling caustic soda type materials.  Personnel should wear rubber globes, apron and eye protection when handling Ambex E-1000.

EQUIPMENT RECOMMENDATIONS:

Processing tanks should be constructed of mild steel.  Heating coils fabricated of mild steel of 300 series stainless steel are satisfactory.

OPERATING INSTRUCTIONS:

Suggested operating conditions are:

IMMERSION

Concentration:	4-8 oz/gal (30-60 G/L)

Temperature:                                    100°-180°F (39-82°C)

Time:	Depends on desired etch

The etch rate of Ambex E-1000 can be increased by raising the temperature, concentration and immersion time.

The information presented herein was prepared by technically knowledgeable personnel, and to the best of our knowledge is accurate and true.  It is not intended to be all-inclusive, and the manner and conditions of use and handling may involve other or additional considerations.