AMBEX AS-98

Ambex AS-98 is a blended powdered acid with inhibitors and deflocculants and a special combination of accelerators, including some fluoride salts.  These accelerators speed attack on rust and scale, while the inhibitors retard attack on the base metal.  While it is designed for use primarily on steel, it may also be used on brass, copper, and zinc alloys.  This results in both longer solution life and a better finish on the work.

Ambex AS-98 is also an effective smut remover.  It may be used without current for the purpose, or with direct current to remove even the most difficult smuts.  Ambex AS-98 is also an effective chromium stripper.

Ambex AS-98 is a dry, white, free-flowing granular material which is practically odorless.  There are none of the safety problems associated with the handling of liquid acids, and no carboys to return.  It may be used for barrel, rack, or basket operations.

Suggested conditions are:

Acid dip for Copper & Brass
8-16 oz/gal
(60-120 G/L)


Room Temperature
15-30 seconds

Acid dip for Steel
12-16 oz/gal
(90-120 G/L)


Room Temperature   

15-30 seconds

Acid dip for Zinc
4-8 oz/gal
(30-60 G/L)


Room Temperature
10-15 seconds

Barrel Pickling of Steel
4 oz/gal
(30 G/L)


150F-160F
10-15 minutes


(65C-70C)

Rust removal from Steel
1-2 lbs/gal
(120-240 G/L)


1130F-160F
3-15 minutes


(55C-70C)

Scale removal from Steel
1-1½ lbs/gal
(120-180 G/L)


120F-160F
1-5 minutes


(50C-70C)

Ambex AS-98 requires acid resistant equipment, preferably polyethylene or PVC.  Heaters or coils should be carbon or teflon.  Lead may also be used with acceptable service life if adequately isolated to prevent any stray or galvanic currents from developing.

CAUTION:

Ambex AS-98 is an acid powder and contains fluorides.  Avoid contact with skin or eyes.  In the event of contact, flush thoroughly with water.  For eyes: Get medical attention immediately.  Inform physician of presence of fluoride.  For skin, if redness or irritation develops, or skin whitens noticeably, get medical attention and inform physician of presence of fluoride.

WASTE DISPOSAL INFORMATION:

Ambex AS-98 solutions may be discarded by neutralizing the acid content in accordance with locally acceptable standards for effluent pH.  Removal of sludge may be necessary due to local restrictions.  Total fluoride content is 3.3% by weight as F.  Ambex AS-98 contains no chromates, phosphates or phenolic compounds.

The information presented herein was prepared by technically knowledgeable personnel and to the best of our knowledge is true and accurate.  It is not intended to be all-inclusive, and the manner and conditions of use and handling may involve other or additional considerations. 

