Ambion Corporation

37 Naugatuck Drive

Naugatuck, CT  06770

(203)723-1437

AMBEX ADS-2023

Aluminum Deoxidizer and Desmutter

For Commercial and Industrial Use Only

Not for Resale

Ambex ADS-2023 is an acidic, liquid, pickling compound designed to remove oxides, tarnish, stains, smut, scale and other acid soluble soils from aluminum and its alloys.  It is used before processes that require a clean, bright active surface such as burnishing, anodizing or conversion coating.  It rapidly desmuts aluminum surfaces after alkaline cleaning or etching.  Working solutions of Ambex ADS-2023 are easily prepared, unaffected by hard water, stable, non-fuming and easy to prepare and maintain.

Properties:

Density (lbs./gal.) ……………………………12.2

Appearance …………………………………. Clear brown syrup

Odor ………………………………………….. Acrid

Flash point …………………………………… non-flammable

pH (5% sol’n in water) ………………………. 0.5

Solubility in water ……………………………. Miscible

Use:

Ambex ADS-2023 should be mixed in room temperature water at a dilution rate of 10 to 20% by volume.  The work and/or the solution should be mildly agitated to promote the brightest possible finish.  All work should be precleaned to thoroughly remove oily soils and then completely rinsed in clean water.  Work should have a water break free surface and be absolutely free of residual detergent.  The solution is applied to the work to be cleaned by tumbling or immersion.  Exposure time is usually less than 5 minutes, although severely adulterated surfaces may require longer exposure.  After treatment, the work should be fully water rinsed to remove any residue that may cause restaining of the surface.

Small aluminum parts, such as rivets and eyelets, can be brightened using Ambex ADS-2023 in a tumbling barrel.  Work should be thoroughly cleaned using an alkaline cleaner and then completely rinsed, then descaled with 3% to 10% solution of Ambex ADS-2023 for 1 to 5 minutes and rinsed completely and dried.

Larger parts that are better handled on fixtures or racks should be treated in a soak bath at an Ambex ADS-2023 concentration of 10% to 20% with mild agitation.  As with tumbling, work must be thoroughly cleaned and rinsed before and after treatment.